## Slide 1: Mechanical and Dielectric Properties of Polymers and Metal-Organic Frameworks
Ricardo Silva Buarque
05/26/2022

## Slide 2: DMAx tutorial
1 - On your home directory, run: wget https://repo.anaconda.com/miniconda/Miniconda3-latest-Linux-x86_64.sh
Alternatively, copy the file /expanse/lustre/projects/csd626/ricardosb/DMAx_TUTORIAL/Miniconda3-latest-Linux-x86_64.sh to your home directory
2 - On your home directory, run: chmod +x Miniconda3-latest-Linux-x86_64.sh
3 - On your home directory, run: bash Miniconda3-latest-Linux-x86_64.sh
4 - Accept all installation requirements from Miniconda with "yes"
5 - Run: source ~/.bashrc
6 - Run: conda create -n cms python=3.9
7 - Run: source activate cms
8 - Run: conda install numpy scipy matplotlib pandas jupyter sklearn
9 - On your home directory, run: git clone https://github.com/sdsc-hpc-training-org/reverse-proxy.git
10 - On your home directory, run: mkdir scripts_YOUR_USERNAME && cd scripts_YOUR_USERNAME
11 - Enter your bashrc file (vi ~/.bashrc) and add the following aliases and exports:
alias jupyter="cd ~/reverse-proxy/ && ./start-jupyter -p 'shared' -d '/expanse/lustre/projects/csd626/YOUR_USERNAME/' -A 'csd626' -b './slurm_expanse/jupyterlab.sh' -I“
alias brc="vi ~/.bashrc"
alias sourcebrc="source ~/.bashrc“
export PYTHONPATH=/home/ricardosb/scripts_YOUR_USERNAME
12 - Inside the created scripts directory, run: git clone https://github.com/rsilvabuarque/DMAx.git
13 - Inside the DMAx directory, run: git checkout ricardo
14 - Inside DMAx/dist, run: pip install DMAx-1.0.tar.gz
15 - Run: jupyter -t 1:00:00
All instructions are in: /expanse/lustre/projects/csd626/ricardosb/DMAx_TUTORIAL/README.md

## Slide 3: Properties studied
Mechanical Loss
  Reasons for studying
    Determining risk of mechanical failure and degradation rate for antennae and high-frequency devices
    Determining mechanical heat generation in high-frequency microchips
Dielectric Loss
  Reasons for studying
    Determining risk of failure and heat generation caused by high-frequency oscillating electric fields

## Slide 4: Mechanical Loss (Theory)
Dynamic Mechanical Analysis: calculates the material’s tendency to store energy elastically vs dissipate energy through heat
  Storage Modulus (G’)
  Loss Modulus (G”)
  Loss Tangent: G” / G’ (tan 𝛿)
Measuring with LAMMPS
  Running an NVT production dynamics with the fix deform wiggle term and saving pressure tensor information
Original stress applied by fix deform
Pressure response captured in LAMMPS output

## Slide 5: Mechanical Loss (DMAx Package)
DMAx: High-throughput python workflow for calculating Dynamic Mechanical Analysis with LAMMPS (EARLY ALPHA!!)
Features: runtime convergence, strain size convergence, error margin analysis, master curve generation
Future features: integration with FireWorks and jobflow (which allows for sequential submission of workflow tasks and GUI visualization of workflow completion), integration with Materials Project and ML model to predict properties of other systems without running MD

## Slide 6: Mechanical Loss (Results)
Loss data agrees in magnitude with currently available work at 25GHz
  However, data trend between 2.5 and 25GHz differs
Stress-strain curve indicates degree of crystallinity
  Stress-strain curve for fully viscous liquids are circle
  Stress-strain curve for fully elastic materials are a line crossing the origin
  Slope of major axis of ellipse = elastic modulus

## Slide 7: Mechanical Loss (Master Curve Results)
Master Curves: based on polymeric trends, allow for estimation of material property values at unmeasurable regimes
  Ultimate goal: validate high-frequency mechanical loss (unmeasurable experimentally) by extrapolating MD data to low frequencies and comparing to experimental data
Current data is either “too-trendy” or not trendy enough
  Either gives a bad extrapolation or does not extrapolate to lower frequencies since shift factors are small
PVDF (amorphous / crystalline) DMA data (tangent)

## Slide 8: Dielectric Loss (Theory 1)
Frequency-dependent dielectric Loss: obtained from the autocorrelation function of the total dipole moment
  Kirkwood-Onsager and Green-Kubo theory -> observe fluctuations on properties in steady-state (equilibrium) to determine non-equilibrium properties of the material
    For dielectric loss: observe fluctuations of dipole moment
    Issue: only able to accurately determine small deviations from equilibrium
Frequency-dependent loss
Static dielectric constant

## Slide 9: Dielectric Loss (Theory 2)
Similar approach to frequency-dependent mechanical loss
  Apply an oscillating E-field -> atoms move due to assigned charges generating a pressure oscillation -> analyze pressure response delay from applied field
  Goal: observe far-from-equilibrium properties
    Ex.: More intense or higher-frequency electric field oscillation
  Limitation: does not work with neutral systems (no movement due to partial charges)
Original E-field signal applied by fix efield
Pressure response captured in LAMMPS output

## Slide 10: Dielectric Loss (Theory 1) (Results)
Correctly predicts trends in the dielectric behavior of PTFE
  Known to have a dielectric loss peak at ~200GHz
  Peak fades as the structure becomes amorphous
    Seen both by approaching temperature to melting point and by designing an amorphous structure
Magnitude seems very off from expected values

## Slide 11: Dielectric Loss (Theory 2) (Results)
Observable shift in response from applied field
  However, several orders of magnitude more lossy than theory 1
Next steps: understand “double frequency issue” and test new, less lossy materials
Small amorphous PTFE (450 atoms) @ 10GHz